## Slide 1
Lithium ion batteries and electrochemical sensors
FOCUS 1
Electrochemical Capacitors
Based on Nanotube Forests
FOCUS 2
Hydrogen Storage Materials
FOCUS 3
Catalyst Materials
SD2: Energy Materials
Ramu Ramachandran
The goal of this SD is to study materials for the generation, conversion, and storage of energy using experimentally validated computational methods.
Notes: In response to ERB comments from last year and as part of our Strategic Planning process, H2 storage was phased out in 2012, and the ongoing work in lithium ion batteries was elevated to the level of a Focus Area.

## Slide 2
Lithium Ion Batteries and electrochemical sensors
LA Tech, Xavier
Electrochemical
Supercapacitors
Tulane, UNO
Catalysts for Energy Applications
LSU, LA Tech, SUBR, Grambling
Energy Materials
CNT forest-based supercapacitors
Stable and high-capacity electrode materials.
YSZ-based exhaust gas sensors.
DFT studies of Fischer-Tropsch catalysis
Nitrogen-doped fullerenes as Pt-substitutes in hydrogen fuel cells.
SD2: Energy Materials
yttria-stabilized zirconia

## Slide 3
Electrochemical
Supercapacitors
Tulane, UNO
Focus 1: CNT-based supercapacitors
Lawrence Pratt
Noshir Pesika
Steve Rick

## Slide 4
Electrochemical capacitors based on carbon nanotube forests show great potential.
A molecular level understanding of the interaction of CNT’s with the electrolyte is needed.
Focus 1: CNT-based supercapacitors
http://mitei.mit.edu/news/novel-ultracapacitor
X. You, M. I. Chaudhari, L. R. Pratt, N. Pesika, K. M. Aritakula, and S. W. Rick, “Interfaces of propylene carbonate, ” J. Chem. Phys. 138, 114708 (2013).
31.4±1.6°
Propylene carbonate droplet contact angle with graphite - experiment
Propylene carbonate droplet contact angle with graphite - simulation.
Notes: Developed computational model that correctly predicts the contact angle of propylene carbonate with graphite.

## Slide 5
Experimentally validated model used to study the interaction of electrolyte with CNT forests under different charge/discharge conditions.
Focus 1: CNT-based supercapacitors
http://mitei.mit.edu/news/novel-ultracapacitor
Computer model: (C2H5)4N+..BF4– in propylene carbonate surrounding a carbon nanotube.
Notes: Tetra-ethyl-ammonium tetrafluoroborate in propylene carbonate (TEABF4/PC).

## Slide 6: The first direct simulation of pore-filling in a CNT supercapacitor
Focus 1: CNT-based supercapacitors
Direct numerical simulation: filling of CNT forest with
electrolyte solution
A molecular level understanding of the distribution of ions in the CNT forest and the charge transfer during charge-discharge cycles has been obtained.
Computer model: (C2H5)4N+..BF4– in propylene carbonate interacting with a carbon nanotube forest.
Notes: Tetra-ethyl-ammonium tetrafluoroborate in propylene carbonate (TEABF4/PC). A realistic pattern of charge density is adopted for the charge tube case .. Uniform charge density along the stem but with realistic charge concentrations on the caps. There are eight (8) C_300 tubes in all calculations here (only four are shown). The radii of the pores is about 1nm.
The graph (lower panel) shows the charge above/below the center plane on the tubes (red) and the ions (black). The ionic charge responds in nanosecond time scales to the step change in the tube charges.
We have now done this on twice the system size . Note the bubble formation as the electrolyte demixes from the propylene carbonate solvent. Such results will form the data-basis of extensive analysis of thermodynamic, transport, stress , and damage of these devices.

## Slide 7
Direct simulation of filling: twice the reservoir size
X. You and L. R. Pratt, preliminary results
Focus 1: CNT-based supercapacitors
See posters (p. 5, 33, 81)
Notes: Double-sized calculation .. Note the absence of bubbles in this case .. Note the weak filling of the pores by ions in the discharged (end frames) cases .

## Slide 8: SD2 Focus 1 Milestones
Milestones | Y1 | Y2 | Y3 | Y4 | Y5
Simulation of pore filling in nanowire capacitors . | X | X | X |  | 
Study chemical damage at elevated electric potentials. | X | X | X |  | 
Optimize computational efficiency of ab initio MD techniques. | X | X |  |  | 
Study role of quantum capacitance in electrochemical capacitance. |  | X | X | X | 
Explore additional nanoforest-based capacitor systems. |  |  | X | X | X
On Track
On Track
Done
Ahead
On Track

## Slide 9
Lithium Ion Batteries
LA Tech, Xavier
Focus 2(a): Li Ion Batteries
Lamar Meda
Ramu Ramachandran
Collin Wick

## Slide 10
Figure 1*: Revenue contributions by different battery chemistries
*Frost & Sullivan (2009)
Need for :
Highly reactive materials with much higher energy and power density
High cyclability- electrodes maintain structural integrity upon multiple charge-discharge cycles
GENERAL INTRODUCTION/MOTIVATION FOR THIS WORK
Focus 2(a): Li Ion Batteries

## Slide 11: Experimental motivation for this work
Balaya et al. Adv. Funct. Mater. 2003, 13, 621-625
1130 mAh/g
Experimental studies on RuO2 nanoparticles reported by Balaya et al.:
  With “deep discharge,” electrodes cycle only twice before losing capacity.
Experimental studies on RuO2 “nanoplates” by Prof. Meda, Xavier University:
  Stopping short of deep discharge, can cycle many times without loss of capacity.
In both cases, the first discharge curve looks significantly different from subsequent discharges, suggesting that some permanent changes occur in the electrode in the first cycle.
Focus 2(a): Li Ion Batteries

## Slide 12
RuO2 Nanoplates Grown by Chemical Vapor Deposition
Field Emission SEM images of RuO2 nanoplates deposited on stainless 304L substrates.
600 nm
50 nm
nanoplates
100 nm
Rutile structure
Focus 2(a): Li Ion Batteries
L. Meda, Xavier University
Notes: RuO2 nanoplates are produced by chemical vapor deposition on stainless steel substrates. The XRD peaks clearly show rutile crystal structure in the deposited material (along with peaks from stainless steel). Field emission SEM images under high magnification show the nanoplate structure. Supported by NSF through PREM (MRSEC at NYU) as well as LA-SiGMA.

## Slide 13: Performance of RuO2 - 1
Capacity is lost readily for the 850 nm nanoplates, but it is lost at a slower rate for the 430 nm ones.
Small materials are easy to model computationally
850 nm stack of RuO2 nanoplates
430 nm stack of RuO2 nanoplates
If you push the electrode to maximum capcaity (i.e., allow voltage to drop to zero …
Focus 2: Li Ion Batteries

## Slide 14: Performance of RuO2 as an electrode material
Rutile structure is observed in the XRD of the pristine electrode, but the oxide layer appear to become amorphous after “deep discharge.”
 Stainless on steel substrates
After 20 cycles
  
Focus 2: Li Ion Batteries

## Slide 15: Performance of RuO2 (contd.)
850 nm stack of RuO2 nanoplates
However, if you stop short of maximum capacity …
No capacity loss is observed
Note: Flat regions at a particular voltage in the discharge curve represent a particular mechanism.
Focus 2(a): Li Ion Batteries

## Slide 16
Focus 2: Li Ion Batteries

## Slide 17
0 Li
8 Li
16 Li
Structures of Lin(RuO2)8 - 1
Pristine Rutile
Intercalation with minimum disruption to Rutile structure
Intercalation with noticeable disruption to Rutile structure

## Slide 18
24 Li input
24 Li converged
24 Li tetragonal
32 Li input
32 Li converged
16 Li converged
Crystalline phase change!
Structures of Lin(RuO2)8 - 2
Hints of conversion!

## Slide 19
Conversion: (RuO2)8 + nLi → (n/2)Li2O + (n/4)Ru + (8 – n/4)RuO2
Intercalation: (RuO2)8 + nLi → Lin(RuO2)8
Unit cell of Li2O
Unit cell of Ru metal
Intercalation of Li in RuO2

## Slide 20
(a) First lithiation
24Li 16Li 8Li 8Li-adj 0Li
The starting RuO2 structures for the first and subsequent discharges are different!
(b) First delithiation
0Li 8Li 16Li 24Li 32Li
Focus 2(a): Li Ion Batteries

## Slide 21
Capacity = 604 mAh/g
Simulations provide nearly quantitative agreement with experimental observations!
Focus 2(a): Li Ion Batteries
Posters:
Metal oxide nanoparticles as electrode materials (p. 85)
RuO2 and other crystalline metal oxides (p. 89)
Capacity = 582-600 mAh/g

## Slide 22
Computational/Experimental voltages and mechanism for reversible charging and discharging for RuO2 anode materials
(a) Calculated first (red) and subsequent (black) discharge of Lin(RuO2)8 up to n = 24 relative to Li/Li+ assuming an intercalation mechanism. The original rutile structure of RuO2 (bottom left) changes irreversibly to tetragonal (top left) during the first cycle and becomes the reference structure for the second and subsequent cycles.
(b) Experimental discharge curves for 850 nm RuO2 nanoplates from Meda et al.
Specific Capacity
604mAh/g
0 Li (rutile)
0 Li (after 1 cycle))
8 Li (during 1st discharge)
24 Li
Focus 2: Li Ion Batteries

## Slide 23
Electrochemical sensors
LA Tech
Focus 2(b): Electrochemical Sensors
Erica Murray
Daniela Mainardi
Weizhong Dai

## Slide 24: Automotive NOx Sensors Murray Research Group
Commercial NOx exhaust gas sensor systems can detect up to 10 ppm.
New emission standards require greater sensitivity.
Conventional NOx Sensor Design:
  Dense electrolyte and porous electrodes architecture
    NOx sensitivity capable down to 10 ppm
Novel NOx Sensor Design:
  Porous electrolyte microstructure with dense electrodes
    Potential for NOx sensitivity down to 1 ppm
  Novel porous microstructure is promising for satisfying future emission standards
NGK commercial NOx Sensor
Research Challenges:
  Achieving ideal porosity
    Excess porosity lowers sensitivity
    Insufficient porosity limits gas diffusion
  Identifying reaction mechanisms impacting sensing
Focus 2(b): Electrochemical sensors
1 cm
Porous YSZ
Au electrodes
Notes: The role of microstructure was investigated for the impedancemetric response of NOx sensors composed of a porous Y-stabilized ZrO2 (YSZ) electrolyte with Au wire electrodes. The NOx sensors fabricated at firing temperatures of 950°C, 1000°C, and 1050°C. Calculations based on SEM images were used to determine the YSZ porosity achieved as a result of the firing temperature. Impedance spectroscopy was used to measure the electrical response of the sensors while operating at 650°C, in gas atmospheres of 0 – 100 ppm NO and NO2, and O2 concentrations ranging from 1 – 18%.

## Slide 25: NOx Sensor Research
Research Highlights:
Greater NOx sensitivity and stability achieved, particularly for NOx concentrations down to 5 ppm as the porosity decreased to 46%.
Dissociative adsorption of O2 appeared to be the dominant rate limiting reaction, based on impedance spectroscopy and modeling results.
The porous YSZ based NOx sensor could be tuned to give a more rapid response.
Research Aim:
  Correlate YSZ synthesis methods to porosity.
  Determine sensitivity of various synthesized YSZ.
500nm
Porous YSZ
Electrolyte
NOx Sensor Performance
(fraction phase angle response)
Typical performance for sensors with 3 different
porous microstructures.
50%
porous
48%
porous
46%
porous
Sensor Response to NO Gas
Image analysis algorithms analyze SEM images,
Provide input to mathematical models that estimate porosity.
Notes: The impedance results showed the YSZ porosity had a strong impact on sensor performance. Overall, the sensor with the lowest porosity (i.e., approximately 46% porous) demonstrated the lowest impedance, higher stability, and greater sensitivity to NO and NO2. In addition, using impedancemetric sensing the response for NOx concentrations ≤ 10 ppm were distinguishable at operating frequencies as high as 40 Hz such that more rapid sensing was possible.
Additional experiments were carried out to determine oxygen partial pressure and temperature dependence. The resulting data was used to assess the reaction mechanism governing the NOx response and the activation energies with respect to porosity. Dissociative adsorption appeared to be rate limiting. The activation energy values tended to decrease with respect to decreasing porosity and increasing NOx concentration.
Overall, the NOx sensor fabricated at 1050C resulting in a porosity of 46% demonstrated the best behavior/performance (i.e., lower activation energy, lower impedance, greater sensitivity and rapid response).

## Slide 26
Kinetics of Nitric Oxide and Oxygen Gases on Porous Y-stabilized ZrO2 based Sensors
Sajin Killa and Daniela Mainardi, Louisiana Tech University
Reaction path: oxygen surface reactions
NO association with adsorbed O2 on a Zr surface site, followed by O2 dissociative adsorption, atomic oxygen diffusion, and further NO2 formation.
Tested on a 56-atom YSZ/Au model cluster (62% YSZ porosity)
Extrapolated data at 62% YSZ porosity (~126 kJ/mol) indicates the calculated barriers are in reasonable agreement with experiments, especially when the RPBE functional is used.
Focus 2(b): Electrochemical sensors
Notes: Experimental activation energies calculated based on data from impedance measurements increased in magnitude with respect to increasing YSZ porosity. Experimental oxygen partial pressure dependence of the sensors suggested that dissociative adsorption was the dominant rate limiting.
The calculated internal energy of activation at absolute zero, DU, and the Gibbs Free energy barrier (internal energy of activation with the thermal corrections to the Gibbs Free energy at different temperatures included), DG(T), for the forward reaction at the PWC/DNP theory level are DU = 156.2 kJ/mol and DG(650°C) = 181.7 kJ/mol (averaged for the 600-700°C temperature range of the experimental work) respectively.
The calculated internal energy of activation and free energy barrier of the reaction seem overestimated at the PWC/DNP theory level when compared to experimental findings, as expected when LDA functionals are used. In order to provide better kinetic results, the structures optimized at the PWC/DNP theory level were used to conduct single point energy calculations at the PW91/DNP, PBE/DNP, and RPBE/DNP theory levels to obtain new DU and DG values for the reaction. Additionally, the temperature corrections used in the calculation of DG in those cases are the ones calculated at the PWC/DNP theory level. Therefore, it is worth to note, that since full geometry optimizations were not perform at these three GGA levels of theory, only trends can be drawn from the results presented in the Table.

## Slide 27: SD2 Focus 2 Milestones
Milestones | Y1 | Y2 | Y3 | Y4 | Y5
Computational study of lithiumion adsorption on metal oxide nanoparticles. |  |  | X |  | 
Computational study of lithium ion adsorption on metal oxide thin films and other promising electrode materials. |  |  | X | X | X
Experimental study of nanostructured metal oxides as potential electrode materials for lithium ion batteries. |  | X | X | X | X
Multi-scale computational modeling of the kinetics and thermodynamics of NOx and O2 reactions on YSZ sensors for vehicle exhaust applications. |  |  | X | X | X
Fabrication and testing of YSZ sensors for NOx and O2 in diesel exhaust streams. |  |  | X | X | X
Update VisTrails so that it can be used for workflow of lithium-ion battery tomography studies. |  |  | X | X | X
Done
On Track
On Track
On Track
On Track
On Track

## Slide 28
Focus 3: Catalysis
Catalysts for Energy Applications
LSU, LA Tech, Southern
Grambling
Daniela Mainardi
Guanglin Zhao
Ramu Ramachandran
Collin Wick
Bin Chen
Barry Dellinger
Les Butler
Naidu Seetala

## Slide 29
Despite their great economic and environmental significance, the catalytic mechanisms of Fischer-Tropsch reactions are not well-understood.
Towards rapid computational evaluation of Fischer-Tropsch catalysts
Shuo Yao, Oneka Cummings, Josh Riggs, Collin Wick and R. Ramachandran
Louisiana Tech University
C = O
+ CO
Metal Surface
Challenge: Very difficult to get good agreement between calculation and experiment for CO binding energies.
Developing computational protocols using DFT functionals developed by Perdew – with some success!
The first and crucial step : CO binding to metal catalyst surface.
Hypothesis: CO binding energies may be one of the diagnostics for the effectiveness of a given FT catalyst metal and its surface morphology.
CO + H2
Black box
of Catalysis
Gasoline CH3-(CH2)x-CH3 + H2O
Focus 3: Catalysis

## Slide 30
Surface | Calculated Adsorption Energy (eV) |  | Experimental* adsorption energy (eV) | Experimental adsorption site | Predicted adsorption site
 | Without BSSE correction | With BSSE Correction |  |  | 
Cu(111) | -1.106 | -0.701 | -0.5(±0.05) | TOP | TOP
Rh(111) | -2.528 | -1.456 | -1.45(±0.14) | TOP | TOP
Pd(111) | -2.151 | -1.572 | -1.48(±0.09) | HOLLOW | HOLLOW
After testing several DFT functionals and computational protocols, we found that the RPBE functional with BSSE correction gave CO binding energies and adsorption sites that agree well with available experimental data for three metals.
Calculations were done with CP2K using a VDZ orbital basis coupled to plane waves.
* F.Abild-Pedersen, M.P. Andersson, Surface Science. 601 (2007) 1747-1753
Wrong trend
Correct trend
Towards rapid computational evaluation of Fischer-Tropsch catalysts
Shuo Yao, Oneka Cummings, Josh Riggs, Collin Wick and R. Ramachandran
Louisiana Tech University
Focus 3: Catalysis

## Slide 31
CO binding energies - very difficult to get agreement with experiments.
Developing computational protocols using DFT functionals developed by Perdew – with some success!
Collaborating with a North Louisiana start-up – Jupiter Fuels (> $3M in venture capital).
Modeling CO binding on catalyst nanowire tips.
CO adsorption on Cobalt nanowire tips
Towards rapid computational evaluation of Fischer-Tropsch catalysts
Shuo Yao, Oneka Cummings, Josh Riggs, Collin Wick and R. Ramachandran
http://www.asi20.com/page9/index.html
Focus 3: Catalysis
CO + H2
Black box
of Catalysis
Gasoline CH3-(CH2)x-CH3 + H2O
C = O
CO

## Slide 32
Core-shell nanoparticles investigated in the context of FTS mechanism
CO bonds strongly to Co top sites in pure Co and in CoNi systems
CO bonds strongly to mixed CoFe hollow sites in CoFe systems
Fischer-Tropsch Synthesis
Fernando Soto, Purnima Kharidehal, Suraj Gyawali and Daniela Mainardi Louisiana Tech University
The energy cost to hydrogenate CO varies as the composition of the nanocluster is tweaked
Co-shell (Fe)-core at a 1:1 ratio shows the most promising result with an energy cost as low as 0.1 eV for the initiation step
Fe is preferred over Ni when used as core element in a Co core-shell catalysts.
Co10(Ni4)
Co10(Fe4)
Focus 3: Catalysis
Notes: In this project, promising stepped–surface catalysts and core-shell Co-containing binary nanocatalysts are studied using electronic structure methods. The ultimate goal is to provide insights into the design of novel catalyst for F-T reactions.
In order to implement the FTS process at a large– scale, two fundamental issues need to be addressed:
Identification of preferred sites (i.e. stepped surfaces, nanocluster surfaces) for catalytic reactions.
Identification of intermediate species and identification of preferred reaction pathways

## Slide 33
Fischer-Tropsch Synthesis
Fernando Soto, Purnima Kharidehal, Suraj Gyawali and Daniela Mainardi Louisiana Tech University
Focus 3: Catalysis
See poster (p. 141)
Notes: In this project, promising stepped–surface catalysts and core-shell Co-containing binary nanocatalysts are studied using electronic structure methods. The ultimate goal is to provide insights into the design of novel catalyst for F-T reactions.
In order to implement the FTS process at a large– scale, two fundamental issues need to be addressed:
Identification of preferred sites (i.e. stepped surfaces, nanocluster surfaces) for catalytic reactions.
Identification of intermediate species and identification of preferred reaction pathways

## Slide 34
Focus 3: Catalysis
Can N-doped C60 replace Pt in hydrogen fuel cells?
Spin-polarized DFT calculations of nitrogen-doped C60 fullerene (N-C60) as a cathode catalyst for hydrogen fuel cells.
Nitrogen-doped fullerenes as fuel cell catalysts
Minimum energy path for H2O formation process on O(1) through (a) direct pathway and (b) indirect pathway; and H2O formation process on O(2) through (c) direct pathway and (d) indirect pathway, on HH Pauling site of N-C60 fullerene. Embedded images show the atomic structures of the initial, intermediate, and final states of the reaction process, respectively.
F. Gao, G.L. Zhao, S. Yang, J. J. Spivey, “Nitrogen-Doped Fullerene as a Potential Catalyst for Hydrogen Fuel Cells”, Journal of the American Chemical Society, 2013, 135, 3315-3318.
Collaboration between LA-SiGMA and DoE EFRC.

## Slide 35: SD2 Focus 3 Milestones
Milestones | Y1 | Y2 | Y3 | Y4 | Y5
Develop force fields with environment-dependent charges for one metal oxide system. | X |  |  |  | 
Use DFT-based ab initio MD and kinetic Monte Carlo methods to study Fischer- Tropsch and related reactions on metal/metal oxide catalytic systems. |  |  | X | X | X
Exploration of spin-state dependent structure and energetics of metal oxide clusters, especially (FeO)n. |  |  | X | X | X
Perform computational modeling of PCDD/PCDF production on metal oxide clusters. |  | X | X | X | 
Develop computational methods for evaluating catalytic sites in carbon nanotubes for hydrogen fuel cells. |  | X | X |  | 
Computational evaluation of nitrogen doped CNT’s and fullerenes as alternatives for platinum in hydrogen fuel cells. |  |  | X | X | X
Done
On Track
On Track
Done
On Track
On Track

## Slide 36: Other notable SD2 accomplishments
Shawn Cole, PhD student at LA Tech received an Indo-US Science and Technology Forum fellowship to visit and work at IIT-Delhi (ethanol fuel cells).
Steve Rick, UNO, received a $450,000 grant from NSF: “The Effects of Charge Transfer on Aqueous and Ionic Systems.”
Daniela Mainardi, LA Tech, receives AIChE Excellence and Service Award; partner in North Carolina A&T NSF CREST Center for biofuels.
LA Tech REU and RET programs (including “STEM Week”) focused on “Energy Materials.”

## Slide 37
X-ray interferometry data and sinusoidal fitting functions.
• Eq 1 is tradition; currently solved with FFT (not robust)
• Eq 3ff is our new algorithm. It is 1000-fold faster than Levenberg-Marquardt, robust, and flexible. Submitted to Rev. Sci. Instr.
• Result of a collaboration with Prof. Warren Johnson, LIGO, LSU
(1)
(2)
(3)
Notes: Grating-based X-ray interferometry yields 3 images simultaneously.
Point to the plot:
absorption image comes from the average X-ray counts
phase contrast image comes from the shift of the sinusoid
small-angle scattering image comes from the amplitude of the sinusoid
Tomography data set has ~1000 interferograms, each taken with a camera with ~1M pixels, for a total of 10^10 interferograms to solve. A fast algorithm is essential. Constrained L-M takes 10 milliseconds; way too slow. Warren Johnson’s LIGO algorithm takes 500 s.
Paper submitted to Rev. Sci. Instr. Talks given at Synchrotron Radiation Instrumentation (held at NIST; travel supported by LaSIGMA) and at ICTMS (Belgium; overhead return supported travel)

## Slide 38
APS: “Fire at the beamline”
X-ray interferometry movies and flame retardants.
On the way to NIST
neutron tomography
“ICTMS” Ghent, Belgium, July, 2013
Ham: neutron tomography and hydrogen storage
Olatinwo: X-ray interferometry movies and flame retardants
Butler: new algorithm for X-ray interferometry
Notes: NIST: LaSIGMA supported our wrap-up neutron imaging at NIST of hydrogen storage (paper submitted). Next NIST imaging will be on batteries (beamtime proposal pending).
Left-Bolaji Olatinwo (chemistry grad student), right-Bradley Wood (was LSU REU undergrad)
APS: LaSIGMA/NSF supported trip for X-ray interferometry imaging of battery and burning flame retardants.
ICTMS: Overhead return supported trip for Bolaji Olatinwo (grad student), Dr. Kyungmin Ham (CAMD tomography staff scientist), and Les. Trip shows high value of international science travel. European, Japan, Australian tomography is quite advanced. Ham and Olatinwo gave posters. Les gave a talk on a new algorithm.